ANALYSIS OF THE EFFECT OF NITROGEN IN SYNTHESIS OF DIAMOND-LIKE FILMS WITH DIFFERENT METHODS OF GAS ACTIVATION [[1]](#footnote-1)\*)

DOI: 10.34854/ICPAF.2021.48.1.133

1Medvedev A.E., 2Emelyanov A.A., 2Yudin I.B., 2Plotnikov M.Yu., 2Timoshenko N.I. and 3Okotrub A.V.

1Institute of Laser Physics SB RAS, medvedev@laser.nsc.ru
2Institute of Thermophysics SB RAS, alemelyanov@gmail.com
3Institute of Inorganic Chemistry SB RAS, spectrum@niic.nsc.ru

In this paper, the effect of nitrogen additions on the synthesis of diamond films with various methods of precursor activation is analyzed: 1) in a microwave plasma at a flow of gases at moderate pressures; 2) in a microwave chamber at low pressure [1]; and 3) in a flow of gases activated by a heated tungsten filament [2].

Nitrogen additions are of interest, because there appear vacancies at nitrogen additions [3] which, at a concentration of more than 0.1%, are of particular importance for thermodynamic stabilization of the structure with respect to the diamond-graphite transition [4], providing CVD growth of diamond in a metastable state. Nitrogen is also the most suitable candidate for the role of a doping agent in obtaining electronic impurity conductivity with a deep donor energy level (of about 1.7 eV). When diamond is used as a low-dimensional system for quantum informatics, nitrogen-vacancy (NV) defects hold much promise. Finally, the addition of nitrogen to the gas mixture accelerates the growth of {100} faces with respect to {111} up to 4 times [5], which allows controlling the structure of diamond crystals in the process of gas-phase chemical deposition.

|  |  |  |
| --- | --- | --- |
| Раман Три графика 0,1 |  |  |
| Fig. 1. SEM images: a) sample no. 543 (without nitrogen); b) sample no. 544 (with the addition of 0.1% nitrogen).Fig. 2. Raman spectrum of a diamond-like film obtained with activation of a gas mixture by a heated tungsten filament. |

The results of measuring the Raman spectrum show that the optimal content of nitrogen in the mixture is not more than 0.1%. Nitrogen addition narrows the diamond line near 1333 cm-1 (in our case from 20 cm-1 to 7 cm-1). The character of the G-line indicates that the graphite that is present is in a highly disordered (soot-like) state. Higher ordering of crystals with the addition of nitrogen is also confirmed by SEM images.

This work was supported by the Russian Foundation for Basic Research (no. 18-29-19069 MK, no. 18-29-19130 MK and no. 19-08-00533) and under state assignment (AAAA-A17-117021750017-0).

References

1. Polyakov O.V., Gorodetsky D.V., Okotrub A.V. Technical Physics Letters, **39** 13 (2013).
2. Emelyanov A.A., Plotnikov M.Yu., Yudin I.B. Technical Physics, **89** (2019) 1891.
3. Davies G., Lawson S., Collins A., Mainwood A., Sharp S. Phyical Review, **B**, 46 (1992).
4. Bar-Yam Y., Moustakas T.D. Nature, **342**, 786 (1989).
5. Yiming Z., Larsson F., Larsson K. Theoretical Chemistry Accounts, **133**, 1432 (2014).
1. \*) [abstracts of this report in Russian](http://www.fpl.gpi.ru/Zvenigorod/XLVIII/Pt/ru/GC-Medvedev.docx) [↑](#footnote-ref-1)