SPECIAL FITURES OF EXPANSION AND HEATING OF CURRENT-CARRYING PLASMA IN THE VACUUM ARC DISCHARGES OF DIFFERENT TYPE

I.A. Krinberg

ISU, Irkutsk, Russia, e-mail: krinberg@physdep.isu.ru

As it is known the plasma emitted from vacuum arc cathode spots, expands with a super-sonic velocity in a cone of half-angle of 30-500. Following evolution of plasma flow shape depends on the discharge macro-parameters which control the variation of cross-section  with a distance . Three characteristic cases demonstrate the power dependence (see a table). A free quasi-spherical expansion (=2) occurs in a low-current arc where the plasma and magnetic pressure do not influence the ion motion. In a case of arc currents A equilibrium between the magnetic and plasma pressures across the plasma flow is reached. The flow confined by a self-magnetic field, has a parabolic shape (=1) [1]. Application of an axial magnetic field to the vacuum arc leads to plasma streaming along a field and a cylindrical channel (=0) is formed [2].

| n | Plasma flow shape | Flow cross-section | Electron temperature | Conditions of realization |
| --- | --- | --- | --- | --- |
| 2 | conic |  |  | A |
| 1 | parabolic |  |  | A |
| 0 | cylindrical |  |  | External magnetic field |

Solving the thermal balance equation for electrons one can obtain the electron temperature distribution  for any value of  (here  results from the boundary condition near cathode). In a table the dependence of is given for the distances where influence of a boundary condition is inessential. It is seen that three modes of plasma expansion into the vacuum ambient may be distinguished: (i) expansion with a cooling at >1, (ii) isothermal expansion at =1, and (iii) expansion with a heating at 10. This conclusion is supported by the measurements of the ion composition controlled by electron temperature: (i) in a low current arc the mean ion charge =1-3 is invariable with a distance from cathode and corresponds to primary ionisation in a near cathode region, (ii) in a high current arc the ion charge increases up to =2-4, (iii) in a vacuum arc in an external magnetic field the ion charge rises up to=3-5.

References

- Krinberg I.A., Zverev E.A. Plasma Phys. Repts., 1999, v.25, No.1, 82-89.

- Krinberg I.A., Tech. Phys. Letters, 2003, v.29, No.6, 504-506.