STUDY OF MICROSTRUCTURE EFFECT ON PROCESSES IN LASER-IRRADIATED FIBROUS AND FOAM-LIKE MATERIALS

T.N. Aliev, A.E. Bugrov, I.N. Burdonskiy, O.L. Dedova, V.V. Dimitrenko, V.V. Gavrilov, A.Yu. Goltsov, A.I. Gromov(, N.G. Kovalskii, S.F. Medovshchikov, E.V. Zhuzhukalo

Science Research Center of Russian Federation Troitsk Institute for Innovation and Fusion Research, Troitsk, Moscow reg., Russia, e-mail: vvgavril@triniti.ru

*P.N. Lebedev Physical Institute of RAS, Moscow, Russia

Experimental study of powerful laser beam interaction with volume-structured low-density media (1-30 mg/cm3) is continued on the “Mishen” facility (SRC TRINITI). The planar samples of agar (randomly distributed thin fibers) and polystyrene (quasi regular foam-like substance) were irradiated in conditions being of interest for a number of scientific and technical problems, including Inertial Confinement Fusion, high energy density physics, development of efficient laser-plasma X-ray sources etc. In experiments the processes of plasma formation and homogenization as well as the processes of energy transport and X-ray conversion efficiency were investigated in dependence on irradiated material microstructure.

All experiments on irradiation of the planar agar-agar (C12H18O9)n and polystyrene foam (CH)n targets were carried out on the “Mishen” facility (Nd-glass laser with an output beam energy E=100 J at (=1.054 (m in a 3 ns pulse).  In most experiments the average laser intensity on irradiated target surface was ~5(1013 W/cm2 (within a focal spot of ~250 (m diameter). The average density of irradiated samples with thickness of 100-1000 (m was varied from 1 mg/cm3 to 20 mg/cm3 for agar and from 10 mg/cm3 to 30 mg/cm3 for polystyrene. Thin Al or Ni foils were usually disposed at the rear surface of low-density porous samples. Complementary X-ray and optical methods were used to diagnose the laser-plasma interaction processes.

The main results are the following:

- pronounced effect of material microstructure onto parameters and dynamics of produced plasma was experimentally revealed. Inside the laser irradiated polystyrene targets the longitudinal size of efficient-absorption zone (with plasma electron temperature of 0.7-0.8 keV) and energy transfer rate (~500 (m and 2(107 cm/s correspondingly) were measured. At the same average density of irradiated samples these values were by a factor of 3-4 larger than those measured inside the agar targets under the same irradiation conditions;

- preliminary experimental data show that the diameter of cells is very important in the process of heat transfer inside the laser-irradiated porous media. In experiments with polystyrene samples of different average density (12 mg/cm3 and 25 mg/cm3) but with the same cell size (~40 (m) the rate of energy transfer in the longitudinal direction is found to be almost independent on density within experimental error;

- experiments with agar samples (~5 mg/cm3) doped with CuCl2 (~5 mg/cm3) show that the electron temperature of plasma created inside the porous samples is somewhat higher (0.7-0.8 keV) as compared to that observed in experiments with Cu foils of solid-state density (0.5-0.6 keV) (the similar effect was found in our previous experiments with doped agar samples of the average density of 2 mg/cm3).

This work was supported by the Russian Foundation for Basic Research (Projects No. 04-02-17335 and 04-02-17336), INTAS (Project No. 2001-0572), and Human Capital Foundation (Grants No. 20 and 26).