ABOUT SOME POSSIBILITIES IN ELECTRIC ARC STUDY OF PROCESSES BY MEANS OF RECORDING INFRA-RED IMAGES

German V.O., Glinov A.P., Golovin A.P., Kozlov P.V., Lyubimov G.A.

Institute of Mechanics Lomonosov Moscow State University, Moscow, Russia, krestytroitsk@mail.ru

Traditionally at examination fast gas - and electrodynamic processes their video recording is used. Such approach is applied and at examination of the processes arising at the considerable current loadings (0.1-0.5 кА), major interelectrode distances (~30-70 mm), and, hence, and the considerable powers (~1-30 kW) in a discharge gap. It leads to powerful radiation of various bands of the electroarc plasma, preferentially in ultra-violet and visible gamuts of wave’s lengths.

Earlier [1-3] by means of a high-speed video shooting discharge images as in the bands adjoining electrodes, and in an interelectrode gap have been gained. The characteristic sites of an electric arc have been scored and features of their shape are studied. To get into understanding of processes occurring in it more deeply other optical methods not destroying its structure can be used. In particular, with that end in view discharge shootings have been spent and in infra-red (IR) gamuts of wave’s lengths, that supplements the effects stated in [4].

Joint scanning of the images gained in visible and IR gamuts of lengths of waves, and the analysis of oscillograms of a current and voltage has allowed to gain as a discharge overall picture, and to fix the image of its interior structure, in usual requirements subjected to "flare" plasma radiation. Possibilities of application of registrars of images in IR gamut of wave’s lengths and for the analysis of processes immediately on graphite electrodes are shown. Heat exchange modes of heated electrode’s bands with space surrounding electrodes and their rather cold interior, far from contact to discharge plasma, fields are tracked. It is shown that because of strong and deep on a body of a carbon anode of a warm-up velocity of cooling of its surface can be slowed down, as at the expense of feed by heat from deep нагретых fields, and because of a thermal emission at proceeding chemical responses. The IR diagnostics of images can (in comparison with video recording) to give more detailed pattern of structure not only interelectrode plasma, but also a thermal field of electrodes, in particular, beforehand to trace on electrodes occurrence of bands of a local heating. Besides thermodiagnostics of images of cooling down electrodes allows (at unknown or incomplete the thermophysical data on them) to fill missing performances of electrode materials.

Authors express gratitude to employees of Applied Mechanics of the Russian Academy of Sciences: A.F. Kolesnikov – for given for experiment carrying out the infra-red equipment and A.N. Gordeyev – for participation in experiment and for consultations on use of applied programs. We are grateful M.A. Mishchuk (Open Society "Pergamum-engineering") for consultations and technical assistance in carrying out of experiments.

References

- German V.O., Glinov A.P., Kozlov P.V., Lyubimov G.A. - Agency of constructional parametres and aerosphere composition on the form of a discharge of electricity // Fluid Dynamics. 2011. № 6. P. 136-145.

- German V.O., Ershov A.P., Kozlov P.V., Lyubimov G.A., Surkont O.S. - The Experimental research of allocation of concentration of charged particles in an interelectrode space of freely burning atmospheric arc // Fluid Dynamics. 2009. №1. p. 142-152.

- German V.O., Glinov A.P., Kozlov P.V., Lyubimov G.A. - Spectral properties of a diffuse-constricted arc discharge // High Temperature. 2012. V.50. №2. p.1.

- German V.O., Glinov A.P., Golovin A.P., Kozlov P.V., Lyubimov G.A. - About some features of visualisation of processes in an extended electric arc in the free atmosphere of air // Applied Physics. 2012. №6. p.1 (in Russian).