INVESTIGATION OF LASER-PLASMA INTERACTION IN EXPERIMENTS WITH LOW-DENSITY VOLUME-STRUCTURED MEDIA ON THE “MISHEN” FACILITY.

A.E. Bugrov, I.N. Burdonskiy, I.K. Fasakhov, V.V. Gavrilov, A.I. Gromov, V.N. Kondrashov, N.G. Kovalskiy, S.F. Medovshchikov, V.G. Nikolaevskiy, M.I. Pergament, V.M. Petryakov, G.M. Yankovskiy, E.V. Zhuzhukalo

TRINIITI, Troitsk, Moscow reg., 142190, Russia, e-mail: vvgavril@triniti.ru

*P.N. Lebedev Physical Institute, 53 Leninskiy prosp., Moscow, 119991, Russia

The new results obtained in experiments on the “Mishen” facility (TRINITI) with laser-irradiated low-density porous media are presented and discussed. Utilization of low-density porous materials as components of various types of laser-irradiated target designs is believed to be the fruitful and promising approach in a number of very important research programs. These materials can provide the uniform energy deposition in direct-drive Inertial Confinement Fusion (ICF), as well as the suppression of high-Z plasma expansion and thus stabilization of X-ray conversion regions in indirect-drive ICF. Application of low-density media seems to be helpful and promising in many other (non ICF) research programs including development of powerful coherent and incoherent X-ray sources, laboratory modeling of astrophysical objects and phenomena, EOS investigations in conditions of extremely high energy densities in different materials.

The variety of optical and X-ray diagnostic methods was used to characterize physical processes in laser-irradiated (=1.054 m, =3 ns, I=1013-1014 W/cm2) plane porous samples of different volume-structure and chemical composition; an average density was varied in the range from 1 mg/cm3 to 10 mg/cm3.

The main results of our experiments are the following:

- the 200–300 m thick agar layer with an average density of 2-3 mg/cm3 deposited on laser irradiated targets of medium- or high–Z elements is shown to suppress efficiently the expansion of X-ray-emitting plasma. The intensity of soft X-ray is about 50% of that measured without agar covering, and it increases up to 70% when agar is doped with CuCl2;

- under the oblique incidence (45) of laser beam onto plane agar targets with average densities in excess of 5 mg/cm3 the hot plasma region formed inside irradiated samples extends along the normal to the target surface, but for agar samples with average densities less then 2 mg/cm3 this region extends along the direction of laser beam propagation, but the energy transport to the target rear side remains quite efficient;

- the plasma formation and energy transport processes is found to differ in laser-irradiated low-density matter of different microstructure (chaotic fibrous structure in agar, quasi-regular cellular structure in polystyrene foam). At the same average density (10 mg/cm3) the longitudinal size of the hot plasma region as well as energy transport rate are significantly higher than observed in agar samples.

This work was supported by the Russian Foundation for Basic Research (Projects No. 01-02-17336 and 01-02-17361) and INTAS (project No. 2001-0572).

Authors

Bugrov A.E. – Russia, Moscow reg., Troitsk, TRINITI, bugrov@aport.ru

Burdonskiy I.N. - Russia, Moscow reg., Troitsk, TRINITI, igb@aport.ru

Fasakhov I.K. - Russia, Moscow reg., Troitsk, TRINITI, fasakhov@triniti.ru

Gavrilov V.V. – Russia, Moscow reg., Troitsk, TRINITI, vvgavril@triniti.ru

Goltsov A.Yu. - Russia, Moscow reg., Troitsk, TRINITI, goltsov@triniti.ru

Gromov A.I. – Russia, Moscow, P.N. Lebedev Physical Institute

Kondrashov V.N. - Russia, Moscow reg., Troitsk, TRINITI, vak@triniti.ru

Kovalskiy N.G. - Russia, Moscow reg., Troitsk, TRINITI, vvgavril@triniti.ru

Medovshchikov S.F. - Russia, Moscow reg., Troitsk, TRINITI

Nikolaevskiy V.G. - Russia, Moscow reg., Troitsk, TRINITI

Pergament M.I. - Russia, Moscow reg., Troitsk, TRINITI, pergam@triniti.ru

Petryakov V.M. - Russia, Moscow reg., Troitsk, TRINITI, vvgavril@triniti.ru

Yankovskiy G.M. - Russia, Moscow reg., Troitsk, TRINITI,vak@triniti.ru

Zhuzhukalo E.V. - Russia, Moscow reg., Troitsk, TRINITI, goltsov@triniti.ru