INVESTIGATION OF HYDRODYNAMIC PROCESSES IN PLANAR TARGETS IRRADIATED BY POWERFUL X-RAY PULSES ON “ANGARA-5-1” FACILITY

V.P. Efremov, I.N. Frolov, V.V. Gavrilov, A.Yu. Goltsov, E.V. Grabovsky, V.N. Kondrashov, G.M. Oleinik, A.I. Potapenko

SRC RF TRINITI, Troitsk, Moscow reg., Russia, e-mail: angara@triniti.ru

*IHED RAS, Moscow, Russia

The experimental and numerical study of the interaction of powerful X-ray pulses with planar targets of different type including low-density (~10 mg/cm3) materials was carried out on the “Angara-5-1” facility. This investigation was initiated with the aim to study the generation and propagation of shock and heat waves in the volume-structured media exposed to extreme-energy load.

Z-pinch discharge with multiwire cylindrical liner was used as a powerful X-ray source in these experiments. The maximum current of 6 MA (at the maximum voltage of 1.5 MV) was obtained in 90 ns-duration pulse providing powerful X-ray pulses. The optical and X-ray diagnostic tools were developed and successfully used to study the processes of energy absorption and transfer inside low-density volume-structured samples and solid-density foils irradiated by the X-ray flux. The parameters of X-ray source were carefully measured with spatial and temporal resolution.

The main results are as follows:

- it was shown that under the real experimental conditions the power flux on the irradiated target surface was ~1012 W/cm2 (X-ray pulse duration – 10-15 ns, quanta energy – 150-1800 eV);

- developed set of diagnostic tools allowed to obtain the preliminary data on the process of powerful X-ray flux interaction with various targets;

- dense low-temperature plasma was observed nearby the target surface 20-30 ns before the driving X-ray pulse;

- the possibility to increase the dynamical contrast ratio of X-ray pulse irradiating the target was demonstrated by use the protective mylar films (1-3 m thick). The power flux density on the irradiated target surface is two-three times less in this case;

- plasma temperature on the irradiated target rear side was estimated to be in the range of 7-12 eV;

- preliminary 1-D hydrodynamic numerical simulations were conducted. Comparison of the experimental and calculated data shows reasonable quality of the physical model used in the simulations.

This work was supported by the Russian Foundation for Basic Research (Project No. 04-02-17341.