STUDY OF PHYSICAL PROCESSES IN LASER-IRRADIATED POROUS TARGETS OF DIFFERENT MICROSTRUCTURE

*N.G. Borisenko, A.E. Bugrov, I.N. Burdonskiy, V.V. Dimitrenko, **A.Ya. Faenov, I.K. Fasakhov, V.V. Gavrilov, A.Yu. Goltsov, A.I. Gromov, A.M. Khalenkov, N.G. Kovalskii, **A.I. Magunov, S.F. Medovshchikov, Yu.A. Merkuliev, B.N. Mironov, **T.A. Pikuz, M.V. Putilin, **I.Yu. Skobelev, E.V. Zhuzhukalo

Science Research Center of Russian Federation Troitsk Institute for Innovation and Fusion Research, Troitsk, Moscow reg., Russia, e-mail: vitaliy@triniti.ru
*P.N. Lebedev Physical Institute of RAS, Moscow, Russia
**Multicharged Ions Spectra Data Center, VNIIFTRI, Mendeleevo, 141570, Russia

Experimental study of powerful laser beam interaction with volume-structured low-density media (1-30 mg/cm3) is continued on the “Mishen” facility (SRC TRINITI). The planar samples of agar and cellulose triacetate (randomly distributed thin fibers) and polystyrene (quasi regular foam-like substance) were irradiated in conditions being of interest for a number of scientific and technical problems, including Inertial Confinement Fusion, high energy density physics, development of efficient laser-plasma X-ray sources etc. In experiments the processes of plasma formation and homogenization as well as the processes of energy transport and X-ray conversion efficiency were investigated in dependence on irradiated material microstructure.

All experiments on irradiation of the porous samples were carried out on the “Mishen” facility (Nd-glass laser with an output beam energy E=100 J at =1.053 m in a 3 ns pulse). In most experiments the average laser intensity on irradiated target surface was ~51013 W/cm2 (within a focal spot of ~250 m diameter). The average density of irradiated samples with thickness of 100-600 m was varied from 1 mg/cm3 to 30 mg/cm3. Thin Al or Ni foils were usually disposed at the rear surface of low-density porous samples. Complementary X-ray and optical methods were used to diagnose the laser-plasma interaction processes.

The main results are the following:

- pronounced effect of material microstructure onto parameters and dynamics of produced plasma was experimentally revealed. Inside the laser irradiated polystyrene targets the longitudinal size of efficient-absorption zone (with plasma electron temperature of 0.7-0.8 keV) and energy transfer rate (~500 m and 2107 cm/s correspondingly) were measured. At the same average density of irradiated samples these values were by a factor of 3-4 larger than those measured inside the agar and cellulose triacetate targets under the same irradiation conditions;

- experiments with fibrous materials of significantly different characteristic scales of structure elements (agar, cellulose triacetate) do not reveal any pronounced effect of structure scale length onto the energy transport rate;

- the intensity dependencies of the electron and ion plasma temperatures are measured in agar targets of ~3 mg/cm3 density for the range of (0.5-5)1013 W/cm2: the electron temperature rises from 0.6-0.7 keV to 0.8-0.9 keV, and the ion temperature rises from 1.0-1.2 keV to 2.6-2.8 keV following intensity increase;

- both the ion and the electron temperatures are found to decrease by a factor of 1.5-2 following a factor of ~3 increase in the target average density (5 mg/cm3 and 15 mg/cm3 ) (I=51013 W/cm2). In all cases the ion temperature exceeds the electron temperature by a factor of 2-3.

This work was supported by the Russian Foundation for Basic Research (Projects No. 04-02-17335, 04-02-17336 and 05-02-16856), INTAS (Project No. 2001-0572), and Human Capital Foundation.