STUDY OF PHYSICAL PROCESSES IN LASER-IRRADIATED POROUS TARGETS OF DIFFERENT MICROSTRUCTURE and chemical composition

*N.G. Borisenko, A.E. Bugrov, I.N. Burdonskiy, V.V. Dimitrenko, V.V. Gavrilov, A.Yu. Goltsov, A.I. Gromov, I.K. Fasakhov, N.G. Kovalskii, S.F. Medovshchikov, Yu.A. Merkuliev, M.V. Putilin, G.M. Yankovskii, E.V. Zhuzhukalo

Science Research Center of Russian Federation Troitsk Institute for Innovation and Fusion Research, Troitsk, Moscow reg., Russia, e-mail: vvgavril@triniti.ru
*P.N. Lebedev Physical Institute of RAS, Moscow, Russia, e-mail: merkuli@sci.lebedev.ru

Experimental study of powerful laser beam interaction with volume-structured low-density media (1-30 mg/cm3) was continued on the “Mishen” facility (SRC TRINITI). The planar samples of agar and cellulose triacetate (TAC, randomly distributed thin fibers) and polystyrene (quasi regular foam-like substance) were irradiated in conditions being of interest for a number of scientific and technical problems, like Inertial Confinement Fusion, high energy density physics, development of efficient laser-plasma X-ray sources etc. In experiments the processes of plasma formation and homogenization as well as the processes of energy transport and X-ray conversion efficiency were investigated in dependence on irradiated material microstructure.  Also started were the experiments on irradiation of the two-to three layer TAC targets with layer densities of 2, 5, and 10 mg/cm2 (with lower density layer located on the laser-irradiated side of the target).

All experiments were carried out on the “Mishen” facility (Nd-glass laser with an output energy E=100 J at =1.053 m in a 3 ns). In most experiments the average intensity on the target surface was ~51013 W/cm2 (within a focal spot of ~250 m diameter). The average density of irradiated samples with thickness of 100-600 m was varied from 1 mg/cm3 to 30 mg/cm3. Thin Al or Ni foils were usually disposed at the rear surface of low-density porous samples. Complementary X-ray and optical methods were used to diagnose the laser-plasma interaction processes.

The main results are the following:

- the experiments with agar and TAC of the same average density in the range of 2-10 mg/cm3 do not reveal any significant difference in the rate of energy transport insider the irradiated samples;

- the X-ray conversion efficiency is measured as dependent on the laser beam intensity at the surface of agar and TAC targets of ~10 mg/cm3;

- in experiments on irradiation of TAC targets doped with high Z element (Cu, 20 weight %, average target density 10 mg/cm3) no significant effect of dopant onto the plasma parameters was found as well as onto the rate of energy transfer;

- grazing incidence spectrometer with spherical diffraction grating was used for measuring the Ni-, Co-, and Fe-like spectra of Sn in the range of 1-20 nm in the set of preliminary experiments on irradiation of agar samples doped with SnO2.  The results of these measurements will be presented elsewhere.

This work was supported by the Russian Foundation for Basic Research (Projects No. № 05-02-16856, 05-02-17275, 06-02-17526, and 07-02-00999).