Strong Microwave Absorption by A filamentary Microwave discharge exited on a dielectric surface

Ivanov V.A., Sakharov A.S., Konyzhev M.E.

A.M. Prokhorov General Physics Institute of Russian Academy of Sciences, Moscow, Russia, sakh@fpl.gpi.ru

Microwave discharges excited by pulsed microwave radiation (2 MW, 2 GHz, 3 s) in a rectangular waveguide (H10 mode) on the surfaces of organic glass targets in vacuum (106 Torr) were studied. Different stages of a surface microwave discharge were observed: secondary-electron-emission microwave discharge, surface microwave breakdown (filamentary discharge), and plasma-flare microwave discharge [1]. It is found that, in the stage of microwave breakdown (which lasts for ~0.1 s), up to 70% of the incident power is absorbed by the dense plasma of a filamentary discharge. According to the Stark broadening of the atomic hydrogen H line ( = 656.3 nm), the electron density in this stage reaches 21018 cm–3 [2], and the electron temperature estimated using the Saha formula is 1.52 eV. Strong interaction of the dense plasma of the filamentary microwave discharge with the dielectric leads to a local destruction of the dielectric surface in the form of a long thin erosion track (l  6 cm, d  100200 m).

An electrodynamic model of the interaction of the waveguide microwave field with a thin cylindrical plasma filament is constructed. The model accounts for the absorption and scattering of the waveguide field by the filament, as well as for reflections of the scattered radiation from the waveguide walls. According to theoretical predictions, the plasma of a filamentary discharge with the above parameters can absorb up to 70% of the incident microwave power, which agrees well with the experimental results.

This work was supported by the Russian Foundation for Basic Research (project no. 09-02-00421-а) and the RF Presidential Program for State Support of Leading Scientific Schools (grant no. 452.2008.2).

References

- Ivanov V.A., Konyzhev M.E., Gavrilenko V.P. et al. Microwave discharges on the surfaces of dielectrics // In book: Microwave Discharges: fundamentals and applications. Ed. Yu.A. Lebedev. Published by “Yanus-K”. Moscow, 2006. P.233-238.

- Ivanov V.A., Konyzhev M.E., Gavrilenko V.P. et al. creation of super dense plasma due to contracting of microwave discharge on surface of dielectric // In book: Strong Microwaves in plasmas. Ed. A.G. Litvak. V.2. P.784-792. Nizhny Novgorod-2005. ISBN 5-8048-0039-X.