LASER INTERACTION WITH FOAM TARGETS

N.G. Borisenko, S. Chaurasia*, L.J. Dhareshwar*, A.I. Gromov, N.K. Gupta*, Yu.A. Merkuliev, D.S. Munda*, V.G. Pimenov**, E.E. Sheveleva**, S. Tripathi*

Lebedev Physical institute, Moscow, Russia, e-mail: ngbor@sci.lebedev.ru
*Laser and Neutron Physics Section, Bhabha Atomic Research Centre, Mumbai-85, India
**Zelinsky Organic Chemistry institute, Russian Academy of Sciences, Russia

Detailed knowledge of laser interactions with low-density porous materials is important for foam employment in the target design that may significantly facilitate various applications of high power lasers. Low-density triacetate cellulose (TAC) targets for laser irradiation are prepared not in the form of textile or artificial fibrous material as most widely used but in the form of well-organized three-dimensional network with even and delicate open-cell structure -  airgel. Along with near-critical density plastic airgel layers “the metal smog” layers formed from metal particles of 0.1µm were fabricated for comparative experiments. These were conducted using intense Nd:Glass laser chain system in BARC. Energy of up to 16 J at 300-800 ps pulse was delivered on the target with a flux of 1013 to 2x1014 W/cm2. The detailed study of plasma under powerful laser shot was performed measuring light transmission and scattering, x-ray and ion emission. Initially microheterogeneous plasma is considered and energy transmittance dependences are measured via areal densities and thickness for several densities. The transparencies within 6% for plasma from plastic airgel are consistent with plasma experiments in the world.

We acknowledge partial support of ILTP A3-41 and RFBR №07-02-01148 projects

References

- Khalenkov A.M., Borisenko N.G., Kondrashov V.N., Merkuliev Yu.A., Limpouch J., Pimenov V.G. Experience of microheterogeneous target fabrication to study energy transport in plasma near critical density. // Laser & Particle Beams, 2006, Vol. 24, pp. 283-290.

- Borisenko N.G., Akunets A.A., Khalenkov A.M., Klir D., Kmetik V., Krousky E., Limpouch J., Masek K., Merkuliev Yu.A., Pfeifer M., Pimenov V.G., Ullschmied J.. Particular features of the transmission of laser radiation with wavelength 0.438 μm and intensity (3-7)∙1014 W/cm2 through an undercritical plasma from polymer aerogels. // Journal of Russian Laser Research. 2007, Vol. 28, No 6, pp. 500-518

- Labaune C, Depierreux S, Tikhonchuk V T, Michel D T, Stenz C, Borisenko N G, Nicolaï Ph, Hüller S, Pesme D, Loiseau P, Masson-Laborde P-E, Casanova M, Grech M, Riazuelo G, Riconda C, Weber S, Darbon S, Wrobel R, Alozy E, Casner A, Meyer C, Romary P, Thiell G, Nazarov W, Limpouch J. Laser-plasma interaction physics in multi kilojoule experiments (in print for IFSA 2009 Proceedings)